# PART 1 - GENERAL

  - Section Includes

Edit acoustical where required

    - Sprayed cellulose Fire [and acoustical] spray material.

# Related Items

    - Inspect all wall assemblies to determine if walls meet the UL 395 specification or any other approved UL assemblies.

# Submittals

    - Submit product data and manufacturer's certificate that the product meets or exceeds specified requirements.

B.	Manufacturer's written certification that product contains no asbestos, fiberglass or other man-made mineral fibers, and free of ammonium based additives.

C.	Copy of manufacturer’s ISO 9001:2008 Certification.

# Quality Assurance

    - Manufacturer must be ISO 9001:2008 Certification.

    - Manufacturer must subscribe to independent laboratory follow-up inspection services of Underwriters Laboratories. Each bag shall be labeled accordingly.

# Delivery, Storage and Handling

    - Deliver in original, unopened containers bearing name of manufacturer, product identification and reference to U.L. testing.

    - Store materials dry, off ground, and under cover.

# PART 2 - PRODUCTS

  - Acceptable Manufacturers

    - International Cellulose Corporation 12315 Robin Boulevard

Houston, Texas 77045

(713) 433-6701 or (800) 444-1252

FAX:  (713) 433-2029

# Materials

    - Celbar RL

      - The sprayed insulation must have been tested in sprayed form by U.L. and have each bag labeled with the reference to U.L. test results according to ASTM E-84/U.L. 723:

        - Tested at a minimum of 4” thickness, Class 1 (A)

        - Flame Spread: 15

        - Smoke Developed: 0

      - Comply with local Building Code Requirements.

      - Fire Rating: 2 Hour UL 395.

# PART 3 - EXECUTION

# Preparation

    - Provide masking, drop cloths or other satisfactory coverings for materials/surfaces that are not to receive insulation to prevent damage from over-spray.

    - Coordinate installation of the sprayed cellulose fiber with work of other trades.

    - Install Celweb as needed. See Tech Bulletin for complete instructions.

# Installation

    - Install spray applied insulation according to manufacturer’s recommendations. Apply material with specially designed nozzle using pressure recommended by the manufacturer.

    - Cure insulation with continuous natural or mechanical ventilation.

    - Remove and dispose of over-spray.

# Protection

A.	Protect finished installation under provisions of Division 1.

END OF SECTION