# PART 1 – GENERAL

  - Section Includes

    - Sprayed cellulose thermal insulation. (07 21 29)

    - Sprayed cellulose acoustical insulation. (09 83 16)

# Related Items

    - Clips, hangers, supports, sleeves and other attachments to spray bases are to be placed by other trades prior to the application of sprayed insulation.

    - Ducts, piping, conduit or other suspended equipment shall not be positioned until after the application of sprayed insulation.

    - Roof penetrations to be installed prior to application.

# Quality Assurance

    - Manufacturer must have a current Underwriters Laboratories (UL) Code Evaluation Report.

    - Manufacturer must be in compliance with the 2009-2021 International Building Code.

    - Manufacturer must be ISO 9001:2015 Certified.

    - Manufacturer must be Forest Stewardship Council (FSC) Chain-of-Custody Certified.

    - Applicator: Licensed by manufacturer.

    - Manufacturer must subscribe to independent laboratory follow-up inspection services of Underwriters Laboratories and Factory Mutual. Each bag shall be labeled accordingly.

    - Mock-up: Apply a 100 square foot representative sample to be reviewed by the Architect and/or Owner prior to proceeding.

    - Manufacturer shall have a minimum 10-year successful performance history of producing and installing spray-applied cellulose on similar projects

    - Material must be tested in accordance with ASTM E 1042 by a NVLAP accredited testing laboratory.

# Submittals

    - Submit product data that the product meets or exceeds the following specified requirements.

      - Bond strength shall be greater than 150 psf per ASTM E 736.

      - Product shall be Class 1 Class A per ASTM E 84/ UL 723.

      - Non-corrosive per ASTM C 1149

      - Bond Deflection per ASTM E 759: 6” Deflection in 10’ Span – No Spalling or Delamination.

      - R-Value to be 3.70 per inch per ASTM C 518.

      - Comply with 2015 IBC Section 803.12 stability requirements for interior finishes.

      - Meet ASTM C 1149

      - Product shall be Cradle to Cradle® Certified v.3.1 or higher to a minimum certification level of Bronze

      - Product shall be UL GREENGUARD Gold Certified

      - Product must have a publicly available Health Product Declaration (HPD) to 100 PPM

      - Product must have a third-party verified, publicly available, product-specific Environmental Product Declaration per ISO 14025

      - Manufacturer's written certification that product contains no asbestos, fiberglass or other man-made mineral fibers.

      - Copy of manufacturer’s ISO 9001:2015 Certification.

      - Minimum Fiber Recycled Content to be 80%.

      - Cannot contain any added Urea-Formaldehyde Resins.

# 1.06 Delivery, Storage and Handling

- Deliver in original, unopened containers bearing name of manufacturer, product identification and reference to U.L. testing.

- Store materials dry, off ground, and under cover.

- Protect liquid adhesive from freezing.

- Water to be potable.

# PART 2 – PRODUCTS

  - Acceptable Manufacturers

    - International Cellulose Corporation 12315 Robin Boulevard

Houston, Texas 77045

Phone: (713) 433-6701 or (800) 444-1252

Fax: (713) 433-2029

Website: www.spray-on.com Email: icc@spray-on.com

    - For approved applicators contact ICC at (800) 444-1252.

# Materials

    - K-13 Spray-On-Systems.

      - Color shall be from Manufacturer’s standard color chart or custom color as noted

      - Each bag must be labeled with appropriate UL classification and FM markings

      - Each drum of adhesive must be labeled “SK-2000 adhesive to be used with K-13”

# PART 3 – EXECUTION

        - Examination

          - Examine surfaces and report unsatisfactory conditions in writing. Do not proceed until unsatisfactory conditions are corrected.

          - Verify surfaces to receive spray insulation to determine if priming/sealing is required to insure bonding and/or to prevent discoloration caused by migratory stains.

# Preparation

          - Provide masking, drop cloths or other satisfactory coverings for materials/surfaces that are not to receive insulation to protect from over-spray.

          - Coordinate installation of the sprayed cellulose fiber with work of other trades.

          - Prime surfaces as required by manufacturer’s instructions or as determined by examination.

          - Prime all gypsum board surfaces with high quality, commercial, gypsum board primer.

# Installation

- Install spray applied insulation according to manufacturer’s recommendations.

- Comply with local Building Code requirements.

- Install spray applied insulation to achieve an average R-Value of 	.

- Install approved 6” stick pins 16” o.c. in both directions, starting 3” from the walls.

- The first pass will be an average of 4” or 5” thick.

- The color for the first pass will be tan.

- Install spray applied insulation to manufacturer’s recommendations.

- Attach Structa-lath III to stick pins with galvanized washers.  Pull any slack from lath.

- Install the second pass of spray-applied insulation to total required R-Value.

- Color to be Light Gray.

- Use fans to keep air moving across the material and force moisture laden air outside.  The material must be ventilated continuously until dry.

- Remove and dispose of over-spray.

# Protection

    - Protect finished installation under provision of Division 1.

END OF SECTION